TRIANGLE POTTERS' GUILD

GLAZE RECIPES

November, 1988

Table of Contents

BLACK GLAZES 	   3

BLUE GLAZES 	   6

BROWN GLAZES 	  10

CELADON GLAZES 	  12

CLEAR/TRANSPARENT GLAZES 	  15

COPPER GLAZES 	  19

CREAM/OFF-WHITE GLAZES 	  24

GREEN GLAZES 	  28

MISCELLANEOUS COLORS 	  32

ORANGE GLAZES 	  38

RED GLAZES 	  41

RED GLAZES (COPPER) 	  45

WHITE GLAZES 	  50

YELLOW GLAZES 	  55

SLIPS 	  58

CLAY BODIES 	  62

NOTES AND TIPS 	  65

ALPHABETICAL LIST OF GLAZES 	  68

INDEX 1 - GLAZES BY COLOR 	  71

INDEX 2 - GLAZES BY TEMPERATURE/FIRING METHOD 	  74

BLACK GLAZES

Cushing Black		Cone 9-10 Reduction

Mary Roehm

Nephelyne Syenite	10.0		Ed Duffield

Albany Slip	65.0

Barium	10.0

Talc	16.0

Chrome	 4.0

Manganese Oxide	 2.0

Cobalt Oxide	 2.0

Smooth waxy black.

K-10		Cone 10 Reduction

White Oak Pottery

Custer Feldspar	5850 grams

Whiting	2290

Kaolin	 700

Silica	3950

Red Iron Oxide	1279

K-10 fires to a gloss black with brown breaks where it is thin.  When used on the inside of a closed or lidded container pinholing occurs, otherwise it is a very reliable glaze.

Rhodes Black		Cone 10 Reduction

John Givvines

Albany Slip	750

Nephelyne Syenite	150

Barium Carbonate	100

Cobalt Carbonate	  5

Manganese Dioxide	  1

Satin Doll  (Matte Black)		Cone 9-10 Reduction

Conrad Weiser

Albany Slip	65

Nephelyne Syenite	15

Barium Carbonate	10

Talc                          10

100

Add:

Iron Oxide	 2

Chrome Oxide	 1

Manganese Oxide	 2

Cobalt Carbonate	 2

BLUE GLAZES

Beautiful Blue		Cone 6 Oxidation

Dawn Hoyle

Custer Feldspar	3150

Gerstley Borate	1800

Flint	1425

Zinc Oxide	 675

Kaolin	 375

Cobalt Carbonate	  38

Red Iron Oxide	 148.5

An old favorite I used years ago - very glossy, very fluid.

Birds Beak Blue		Cone 10 Reduction

NCSU Craft Center

3.4 kg    6.8 kg

EPK	400       800

Flint                        1000      2000

Whiting	600      1200

Custer Feldspar	800      1600

Talc	400       800

----      ----

Total                      3200      6400

Rutile	160       320

Cobalt Carbonate	 40        80

Blue Break Up 		Cone 5-6 Oxidation

Sandy Brunner

Cornwall Stone	60%

Gerstley Borate	40%

Cobalt	 0.5%

Rutile	 2.5%

Applied thick - gives a nice mottled blue.  Applied over dark brown glazes, it runs - beautiful.

Blue Olive		Cone 10 Reduction 			   or Oxidation

Sertoma Arts Ctr.

Custer Feldspar	45		Dawn Hoyle

Cornwall Stone	22

Kaolin	13

Whiting	20

Cobalt Carbonate	 0.5

Red Iron Oxide	 2

Rutile	 2

Turner Blue		Cone 10 Reduction

NCSU Craft Center

1.2 kg    2.5 kg    5.0 kg

EPK	230       460       920

Nephelyne Syenite	306       612      1224

Cornwall Stone	242       484       968

Whiting	110       220       440

Dolomite	132       264       528

Talc	 76       152       304

Flint	152       304       608

----      ----      ----

Total                      1248      2496      4992

Cobalt Carbonate	 18        36        72

Chrome Oxide	  6        12        24

Vera Blue		Cone 10 Reduction

NCSU Craft Center

2 kg    4.1 kg    6.2 kg

Kingman Feldspar	120      2400      3600

Dolomite	100       200       300

Gerstley Borate	400       800      1200

EPK (Calcined)	150       300       450

EPK (Raw)	150       300       450

----      ----      ----

Total                      2000      4000      6000

Rutile	 80       160       240

BROWN GLAZES

Albany Dark Brown		Cone 10 Reduction

NCSU Craft Center

Barnard Clay	 700	  Dawn Hoyle

Albany Slip Clay	1395

Cornwall Stone	  80

Ball Clay	  30

Flint	  82.5

Whiting	  27.5

Zinc Oxide	  15

Gerstley Borate	 170

CELADON GLAZES

Alfred L. Celadon		Cone 10 Reduction

Mary Roehm

Potash Feldspar	 19		Ed Duffield

Soda Feldspar	 15

Whiting	 17

Barium	  3

Ball Clay	 15

Flint	 31

Red Iron Oxide	  3.0%

Bentonite	  2.0%

Epsom Salt	  0.5%

Nice waxy green celadon.

Celadon		Cone 10 Reduction

NCSU Craft Center

1 kg    3.1 kg    5.2 kg

Custer Feldspar	 278       834      1390

EPK	 203       609      1015

Flint	 346      1038      1730

Whiting	 200       600      1000

----      ----      ----

Total	1027      3081      5135

Red Iron Oxide	   5        15        25

Light green celadon.

Choy Blue Celadon		Cone 10 Reduction

Mary Roehm

Potash Feldspar	61.2		Ed Duffield

Whiting	 7.5

Kaolin	 4.9

Flint	24.8

Barium	20.0

Red Iron Oxide	 2.5

Grey-blue waxy.

Foundry Celadon		Cone 10 Reduction

Mary Roehm

Flint	 84		Ed Duffield

Potash Feldspar	132

EPK	 30

Whiting	 59

Red Iron Oxide	  8

Bentonite	  9

T-14 Celadon		Cone 10 Reduction

Mary Roehm

Potash Feldspar	37.5	 	Ed Duffield

Flint	26.0

Kaolin	15.6

Talc	 6.5

Whiting	14.3

Tin (or Zircopax)	 5.0

Red Iron Oxide	 2.0

CLEAR/TRANSPARENT GLAZES

Clear Glaze                                   Raku

Chris Stanley

Colemanite (Gerstley Borate)  80-75%

Nephelyne Syenite   	20-25%

Makes a nice clear glaze that will hold onto some of the smoke.

I use this as a base to add 5-10% oxides to paint colors on raku.

Georgia Clear		Cone 10 Reduction

Mary Roehm

Potash Feldspar	30		Ed Duffield

Ball Clay	20

Whiting	20

Flint	30

For blue add:

Copper Carbonate	 0.00125  (1/8 of 1%)

Chrome	 0.00125  (1/8 of 1%)

Leach's Transparent Base		Cone 9-10 Reduction

White Oak Pottery

Custer Feldspar	4000

Whiting	2000

Kaolin	1000

Silica	3000

Light celadon:

Red Iron Oxide	   2.0%

Olive Celadon:

Black Iron Oxide	   2.0%

Transparent Gloss Blue:

Black Iron Oxide	   2.0%

Cobalt Oxide	   0.5%

Opaque Gloss White:

Zircopax	  10.0%   or   Tin Oxide     10.0%

(We substitute half of the Tin Oxide with Zirconium Oxide to

help reduce costs.)

Leach's is an extremely reliable and versatile glaze.  It works best when applied thick and doesn't run.  It works well with brushed or sprayed oxide decorations.

Raku Base Glaze                               Raku

Conrad Weiser

Frit # 25                     42.5

Frit # 3134     	27.4

Lithium Carbonate	 9.8

EPK 	 6.3

Silica               	14.0

CMC or gum	 1 tsp/Kg.

Bentonite	 2%

Is clear, gives crackles, good over or under glaze colors.

Raku Transparent                              Raku

Conrad Weiser

Gerstley Borate               76

Nephelyne Syenite             24

CMC       tsp.                 1

Bentonite                      2

Dry mix, then add CMC and water.  Mill for 15 minutes after slaking.

#13 Transparent		Cone 10 Reduction

NCSU Craft Center

1 kg    3 kg     6 kg

Custer Feldspar	285     855     1710

Ball Clay	195     385     1170

Whiting	195     385     1170

Flint	325     975     1950

----    ----     ----

Total                      1000    3000     6000

COPPER GLAZES

Aurora Copper Luster	                Raku

Edge Barnes

Borax	60

EPK	40

Add:

Red Copper Oxide	 8.5%

Manganese Dioxide	 9.0%

Mix borax and EPK into a paste.  Add colorants.  Fire in heavy reduction.

Copper Colemanite		Cone 4-5 Oxidation

Sandy Brunner

Calcined Feldspar	46.8%

Flint	20.0%

China Clay	 2.5%

Whiting	 8.3%

Colemanite (Gerstley Borate)	13.7%

Zinc Oxide	 4.0%

Dolomite	 6.0%

-----

101.3%

Black Copper Oxide	 5.0%

Cone 4 - Matte turquoise

Cone 5 - Semi-gloss turquoise

Cone 6 - Electric blue glossy

By varying the amount of Black Copper Oxide the color can vary from turquoise green to black that breaks to purple and pink.

Copper Luster	                Raku

Tony Marsh

Frit #54	75

Kaolin	15

Zircopax	10

Add:

Copper Carbonate	 3%

Borax	 1%

Copper Matte                                  Raku

Jennie Bireline

Copper carbonate          	90%

Ferro 3110 	10%

Lithium Glaze	                Raku

Tony Marsh

Lithium Carbonate	27.7

Kaolin	14.0

Silica	55.4

Bentonite	 2.9

Add:

Copper Carbonate	 3.8%

Lizard Skin		Raku

Chris Stanley

Colemanite	50		Tony Marsh

Borax	50

Add:

Rutile	10%

Copper Carbonate	10%

Very runny.

LMG		Cone 6 Oxidation

Conrad Weiser

Semi-Matte

Glossy     Semi-Mottled     Matte

Lithium Carbonate	14.0          9.8           7.8

Kingman Feldspar	27.2         27.2          27.2

Whiting	14.8         14.8          14 8

EPK	12.8         12.8          12.8

Flint                         31.2         35.4          37.4

100.0        100.0         100.0

Add:

Copper Carbonate	 2%           2%            2%

Be careful and test well on your clay body.  It shivers sometimes on some clay bodies.

Val's Copper Luster	               	Raku

Edge Barnes

Colemanite	80		Val McGaughey

Soda Feldspar	20

Add:

Copper Oxide	50%

Heavy reduction produces metallic copper.  Turns jade green in oxidation.

Weiser Rust		Raku

Edge Barnes

* Volume Measure *

Colemanite	 5.5

Nephelyne Syenite	 1.25

Copper Carbonate	 1.875

Black Nickel Oxide	 0.5

Tin Oxide	 0.5

* Volume Measure *

Willie Hillix		Cone 10 Reduction

Mary Roehm

Nephelyne Syenite	2500		Ed Duffield

Flint	1400

Whiting	1200

Kaolin (Tile 6)	 700

Bentonite	 150

Copper Carbonate	  50

Black Copper Oxide	 250

Green - red - blue - black.

CREAM/OFF-WHITE GLAZES

Buttercream		Cone 10 Reduction

John Givvines

Feldspar - G200	164

Gerstley Borate	 48

Dolomite	 28

Talc	 30

Kaolin	 20

Flint	 80

Manganese Dioxide	 14

Buttermilk		Cone 10 Reduction

John Givvines

Gerstley Borate	210

Dolomite	136

Whiting	180

Feldspar	586

Kaolin	136

Talc	270

Flint	482

Crane  (Matte)		Cone 9-10 Reduction

or Oxidation

Sertoma Arts Ctr.

Dolomite	18		Dawn Hoyle

Talc	 6

F-4 Feldspar	42

Ball Clay	 8

Flint	26

Ilmanite	 5

Also called 'Speckled Crane'.  Off-white color with tiny dark specks - like the bird's egg.

Hymen's Basic Matte		Cone 10 Reduction 			   or Oxidation

Dawn Hoyle

F-4 Feldspar	 90

Dolomite	110

Kaolin	 90

Whiting	 30

Flint	 25

Can be used on either porcelain (a creamy color) or stoneware (yellow with brown spots).  I use this in reduction firing, but others have used it in oxidation.

Moonglow		Cone 10 Reduction

NCSU Craft Center

2 kg    3.7 kg    5.6 kg

Kingman Feldspar	 760      1520      2280

EPK	 380       760      1140

Dolomite	 340       680      1020

Whiting	  70       140       210

Flint	 160       320       480

----      ----      ----

Total	1710      3420      5130

Superpax	 130       260       390

Bentonite	  10        20        30

Oatmeal		Cone 9-10 Reduction

or Oxidation

Sertoma Arts Ctr.

Custer Feldspar	35	  Dawn Hoyle

Dolomite	20

Kaolin	22.5

Whiting	 3

Talc	19

SLG 25 Tan		Cone 10 Reduction

John Givvines

Albany Slip	30

Nephelyne Syenite	30

Whiting	14

Rutile	10

Flint	 9

Bentonite	 1

SLG 30 Matte		Cone 10 Reduction

John Givvines

Albany Slip	64

Feldspar	34

Rutile	 2

Bentonite	 2

SLG 30 Satin

Substitute Nephelyne Syenite for the Feldspar.

Tan		Cone 10 Reduction

John Givvines

Dolomite	146.4

Feldspar - G200	156.8

Kaolin	136

Nephelyne Syenite	150

Red Iron Oxide	 11.2

Rutile	  4.2

Superpax	115

Best if overlapped - lighter in color if thick.

GREEN GLAZES

Behrens Spinach Green		Cone 5-6 Oxidation

Conrad Weiser

Gerstley Borate	50

EPK	15

Silica	35

Add:

Chromium Oxide	 2%

Glossy with 2 or 3 dips.  Without the Chromium Oxide, this base glaze will give other colors:

Cobalt Carbonate  .25 to 3%  -  Blue

Iron Oxide          3 to 9%  -  Brown

Copper Carbonate    1 to 3%  -  Green

Grass Green		Cone 10 Reduction

John Givvines

Feldspar - G200	848

Kaolin	400

Whiting	354.8

Red Iron Oxide	 81.6

Talc	 64

Marianne Green		Cone 10 Reduction

John Givvines

Feldspar	455

Whiting	 65

Kaolin	 52

Bone Ash	 91

Flint	195

Bentonite	 25

Talc	 52

Red Iron Oxide	 19

Apply thickly.

Peacock		Cone 10 Reduction

John Givvines

Soda Feldspar	367.5

Talc	122.5

Flint	161

Gerstley Borate	108

Dolomite	 56

Kaolin	 40

Green (Peacock)

Chrome Oxide	  6

Red Iron Oxide	  4

Cobalt Oxide	  1

Blue (Peacock)

Cobalt Oxide	  4.2

Chrome Oxide	  4.2

Red Iron Oxide	  4.2

MISCELLANEOUS COLORS

Alice		Cone 10 Reduction

John Givvines

Dolomite	60

Kaolin	50

Cornwall Stone	40

Spodumene	40

Flint	10

Alp		Cone 10 Reduction

John Givvines

Feldspar	57

Kaolin	57

Zinc	10

Dolomite	30

Ball Clay	30

Whiting	20

Titanium	 4

Red Iron Oxide	 4

Ilmanite	 4

Chuck Hindes Shino		Cone 10 Reduction

Mary Roehm

Soda Feldspar	 60	  Ed Duffield

Spodumene	 52

EPK	 12

Soda Ash	 12

Nephelyne Syenite	200

Ball Clay	 68

D 9		Cone 10 Reduction

John Givvines

Dolomite	155

Whiting	 20

Feldspar	125

Kaolin	160

Flint	 35

Red Iron Oxide	  5

Druckman		Cone 10 Reduction

John Givvines

Feldspar	1262

Kaolin	2270

Talc	 908

Flint	 908

Whiting	 454

Dolomite	 454

Guston Shino		Cone 10 Reduction

Mary Roehm

Spodumene	15.2		Ed Duffield

F-4 Feldspar	10.8

Soda Ash	 4.0

EPK	10.0

Ball Clay	15.0

Nephelyne Syenite	45.0

Grey - white - orange.

Honey  (Heavy Iron)		Salt, Cone 8-10

Conrad Weiser

Custer Feldspar	31.6

Flint	20.4

EPK	15.0

Whiting	13.3

Iron Oxide	 7.1

Rather unpleasant if not fired in salt kiln.

Honey		Cone 10 Reduction

John Givvines

Feldspar	1248

Whiting	 216

Zinc Oxide	 196

Barium Carbonate	 504

Ball Clay	 240

Rutile	  48

Red Iron Oxide	  72

Bentonite	  12

Pumpkin		Cone 10 Reduction

NCSU Craft Center

2.3 kg    4.6 kg    6.9 kg

Custer Feldspar	1054      2108      3162

Talc	  80       160       240

EPK	 500      1000      1500

Whiting	 426       852      1278

Bone Ash	  60       120       180

----      ----      ----

Total	2120      4240      6360

Red Iron Oxide	  80       160       240

Rutile	  80       160       240

Bentonite	  40        80       120

Pumpkin		Cone 10 Reduction 			   or Oxidation

F-4 Feldspar	45.4		Dawn Hoyle

Talc	 3.4

Kaolin	21.5

Bone Ash	 2.6

Whiting	18.4

Red Iron Oxide	 3.4

Rutile	 3.4

Bentonite	 1.7

I find this glaze a little dull by itself, but it works very well under and over other glazes to highlight an area or give some variation to color.

Simmon		Cone 10 Reduction

John Givvines

Feldspar	70

Flint	14

Whiting	14

Bentonite	 3

Rutile	 3

Red Iron Oxide	 2

Shino #3		Cone 10 Reduction

Mary Roehm

Custer Feldspar	560		Ed Duffield

Spodumene	480

EPK	176

Soda Ash	128

Shino #5		Cone 10 Reduction

Mary Roehm

Soda Feldspar	 18		Ed Duffield

Spodumene	 16

Kaolin	  2

Nephelyne Syenite	 45

Soda Ash	  4

Ball Clay	 15

Stanley Base Glaze - 1185		Cone 7-9 Oxidation

Chris Stanley

Cornwall Stone	500

Wollanstonite	360     or  Whiting   225

Flint     135

Kingman Feldspar	260

Colemanite (Gerstley Borate)	200

Nephelyne Syenite	200

Spodumene	160

Talc	160

Dolomite	 80

China Clay (EPK)	 60

Bentonite	 20

Flint	245

Stanley Base Glaze - 1185 (cont.)

Colorants:

White:

Tin Oxide	 10%

White pink blush:

Tin Oxide	 10%

Titanium Oxide	  2%

Green:

Chrome or Nickel Oxide	  2%

Blue:

Cobalt Oxide	  0.25%

Brown/green:

Red Iron Oxide	  5%

Black Manganese Dioxide	  3%

Yellow:

Red Iron Oxide	  6%

Black:

Cobalt Oxide	  0.5%

Manganese Dioxide	  4.0%

Blue green:

Cobalt Carbonate	  0.5%

Copper Carbonate	  2.0%

A thick opaque glaze with good colors.  This glaze is from a high school ceramics class - developed for the electric kiln.

Stoney Matt		Cone 10 Reduction

John Givvines

Cornwall Stone	48

Nephelyne Syenite	33

Whiting	 7

Dolomite	26

Talc	27

Kaolin	48

Yanagihara		Cone 10 Reduction

John Givvines

Feldspar	385

Flint	269

Whiting	163

Talc	125

Kaolin	 30

Bentonite	 30

ORANGE GLAZES

Orange 1		Cone 10 Reduction

John Givvines

Feldspar - G200	1569

Kaolin	 640

Dolomite	 608

Whiting	 128

Superpax	 512

Bentonite	  64

Red Iron Oxide	  64

Tin Oxide	  64

Rutile	  16

Orange 2		Cone 10 Reduction

John Givvines

Feldspar	50

Kaolin	50

Dolomite	50

Whiting	10

Bone Ash	 8

Superpax	 8

Rutile	 2

Red Iron Oxide	 1

Orange 3		Cone 10 Reduction

John Givvines

Feldspar	162

Dolomite	 54

Whiting	  9

Kaolin	 75

Red Iron Oxide	  4

Superpax	  5

Reitz Orange		Cone 10 Reduction

John Givvines

Feldspar	240

Whiting	 80

Nephelyne Syenite	 60

Kaolin	 60

Barium Carbonate	 30

Rutile	 30

Red Iron Oxide	 10

Shaner Orange		Cone 9-10 Reduction

Dawn Hoyle

F-4 Feldspar	50

Kaolin	24

Whiting	21

Bone Ash	 3

Talc	 4

Red Iron Oxide	 4

Rutile	 4

Most dependable orange glaze I've used.

RED GLAZES

Flame		Cone 10 Reduction

John Givvines

Feldspar	60

Spodumene	40

Dolomite	45

Kaolin	50

Whiting	 8

Superpax	10

Iron Red		Cone 10 Reduction

Dawn Hoyle

Custer Feldspar	27.9

Dolomite	14.4

Tennessee Ball Clay	13.3

Flint	13.9

Bone Ash	16.4

Red Iron Oxide	14.0

This glaze should be applied thinly.  It's good on stoneware and porcelain.  Can be fired anywhere in kiln, but does best in cold spots with less reduction.

Joan's Plum		Cone 10 Reduction

John Givvines

Soda Feldspar	214.6

Flint	190.8

Kaolin	 54.8

Black Iron Oxide	 11

Red Iron Oxide	 54.4

Whiting	 84

Color is close to Temmoku, but with purple hue sometimes.  Sometimes develops crystals.

Ohata Red		Cone 10 Reduction

NCSU Craft Center

2 kg      4 kg      6 kg

Kona F-4 Feldspar	 880      1760      2640

EPK	 114       228       342

Whiting	 130       260       390

Talc	 114       228       342

Flint	 390       780      1770

Bone Ash	 180       360       540

----      ----      ----

Total	1808      3616      6024

Red Iron Oxide	 194       388       582

Bentonite	  40        80       120

Persimmon		Cone 10 Reduction

John Givvines

Bentonite	 125

Bone Ash	 455

Feldspar - K200	2274.2

Flint	 975

Kaolin	 260

Red Iron Oxide	 585

Talc	 260

Whiting	 325

Plum		Cone 10 Reduction

John Givvines

Cornwall Stone	250

Albany Slip	550

Red Iron Oxide	110

Whiting	100

Temokuse (Iron Saturate)		Cone 10 Reduction

NCSU Craft Center

1.1 kg    3.4 kg    5.7 kg

Custer Feldspar	400      1200      2000

Flint	300       900      1500

Whiting	200       600      1000

EPK	100       300       500

----      ----      ----

Total                      1000      3000      5000

Red Iron Oxide	140       420        700

RED GLAZES (COPPER)

Chun Red		Cone 10 Reduction

John Givvines

Feldspar	374

Kaolin	155

Whiting	127

Dolomite	 62

Titanium	 13

Barium Carbonate	 99

Tin Oxide	 10

Copper Carbonate	 10

Red Iron Oxide	  5

Copper Red #1		Cone 10 Reduction

John Givvines

Feldspar	6390

Kaolin	 222

Flint	3994

Whiting	 399

Gerstley Borate	1331

Dolomite	1331

Zinc Oxide	 266

Barium Carbonate	 665

Tin Oxide	 399

Copper Carbonate	  75

Flambe		Cone 10 Reduction

John Givvines

Feldspar	1440

Kaolin	 500

Flint	 900

Whiting 	  90

Gerstley Borate 	 300

Dolomite	 300

Zinc Oxide	  40

Barium Carbonate	 150

Tin Oxide	  90

Copper Carbonate	  15

Variation:

Red Iron Oxide	  50

Zinc Oxide	  50

Funny Runny Bunny		Salt, Cone 10

Conrad Weiser

Buckingham Spar	330

Kaolin	 17

Flint	312

Whiting	 31

Gerstley Borate	104

Dolomite	104

Zinc Oxide	 20

Barium Carbonate	 52

Tin Oxide	 31

Copper Carbonate	 10

May be red with pink spots, occasionally cloudy or clear.  Risky, but sometimes worth the trouble.  For salt firings only.

G 203		Cone 10 Reduction

John Givvines

Flint	3090

Soda Feldspar	2721

Whiting	1288

Frit 3195	1181

Superpax	 794

Kaolin	 554

Dolomite	 197

Zinc Oxide	  86

Copper Oxide	  79

King Red 1		Cone 10 Reduction

John Givvines

Feldspar	 439

Flint	 181

Whiting	 204

Kaolin	  37

Ball Clay	 113

Tin Oxide	  11

Copper Carbonate	   6

King Red 3		Cone 10 Reduction

John Givvines

Feldspar	 530

Flint	 170

Whiting	 150

Kaolin	  60

Talc	  40

Zinc Oxide	  50

Tin Oxide	  10

Copper Carbonate	   3

Oxblood		Cone 10 Reduction

John Givvines

Nephelyne Syenite	1663

Feldspar	 358

Flint	  77

Gerstley Borate	 887

Whiting	 515

Copper Carbonate	  11

Tin Oxide	  39

Oxblood 2		Cone 10 Reduction

John Givvines

Soda Feldspar	3010

Gerstley Borate	 412

Whiting	 450

Copper Carbonate	  11

Tin Oxide	  39

Red #1		Cone 10 Reduction

John Givvines

Nephelyne Syenite	2069

Gerstley Borate	 463

Whiting	 402

Flint	 822

Copper Carbonate	  14

Tin Oxide	  37

Red #2		Cone 10 Reduction

John Givvines

Feldspar	311

Flint	294

Gerstley Borate	141

Zinc Oxide	 83

Barium Carbonate	 67

Talc	 64

Copper Carbonate	 20

Tin	 15

WHITE GLAZES

"A" Glaze		Cone 5-6 Oxidation

Conrad Weiser

Potash Feldspar	41.3

Whiting	14.9

Zinc Oxide	12.0

EPK	 4.9

Silica	26.9

Titanium Dioxide	 5.0

This is a white basic glaze which will show texture nicely.  Two or three dips gives a glossy surface.  Is especially attractive over an albany slip underglaze decoration.

With colorant additions	             you get:

Nickel Oxide       	0.5 - 5%       	Varying degrees 		 of greenish cream.

Cobalt Carbonate	0.25 - 3%	Light to dark blue.

Copper Carbonate	0.5 - 3%	Light to med green.

Iron Oxide	3 - 9%	Buff to brown.

Cobalt Carbonate 	0.5% 	Robin's egg blue.

Copper Carbonate	2.0%

Cobalt Carbonate	0.25%	Bright blue.

Copper Carbonate	2.0 %

Best Possible White		Cone 10 Reduction

John Givvines

Kaolin	100

Ball Clay	100

Nephelyne Syenite	500

Flint	100

Gerstley Borate	100

Talc	100

Zinc Oxide	 15

Edge's White (maybe clear)		Raku

Edge Barnes

Gerstley Borate	50

Nephelyne Syenite	20

Georgia Kaolin	10

Kona F-4 Feldspar	20

Ferguson White		Cone 10 Reduction

NCSU Craft Center

1.1 kg    3.4 kg    5.7 kg

Custer Feldspar	500      1500      2500

EPK (Calcined) 	120       360       600

EPK (Raw)	120       360       600

Dolomite	160       480       800

Whiting	100       300       500

----      ----      ----

Total                      1000      3000      5000

Tin Oxide	 50       150       250

Bone Ash	 80       240       400

Matte & White		Cone 6 Oxidation

Conrad Weiser

Potash Feldspar (Custer)	51.6

Flint	 5.6

Whiting	18.8

Zinc Oxide	 8.6

EPK                           15.4

100.0

Temple White		Cone 10 Reduction

Dawn Hoyle

G-200 Feldspar	35

Dolomite	19.7

Whiting	 2.6

Kaolin 	22.6

Flint	20

Bentonite	 2

This is my basic white glaze which fires to a grayed white in heavy reduction.  it is very stable and does not move.  I've recently started using G-200 spar instead of Custer spar, the original ingredient, because G-200 is so much cheaper here in N.C.

* According to Ceramics Monthly (Feb. '84), Rick Berman uses this glaze for Cone 9 oxidation firing by changing the Kaolin to Kentucky Ball Clay in the same amount.  He also opacifies this glaze with the addition of 10% Zircopax.

Variation:

Blue

1 Gal.  Temple White

2 Tbsp. Red Iron Oxide

2 Tbsp. Cobalt Carbonate

White Liner		Cone 10 Reduction

Dawn Hoyle

F-4 Feldspar	41

Gerstley Borate	12

Dolomite	 7

Talc	15

Ball Clay	 5

Flint	20

Zircopax	20

This is a satin, shiny glaze that is especially good for the inside of casseroles, teapots, etc.

YELLOW GLAZES

Bringle Yellow		Cone 9-10 Reduction

or Oxidation

Sertoma Arts Ctr.

Custer Feldspar	40		Dawn Hoyle

EPK	25

Whiting	 4

Dolomite	22

Rutile	 5

Mead  (Yellow)		Cone 10 Reduction

John Givvines

Feldspar - G200	425

Barium Carbonate	230

Superpax	180

Dolomite	166

Ball Clay	120

Flint	 45

Gerstley Borate	 11

Red Iron Oxide	 27

Mustard		Cone 10 Reduction

John Givvines

Feldspar	98

Whiting	36

Kaolin	30

Rutile	18

Zinc Oxide	10

Red Iron Oxide	 8

SLIPS

Bringle Slip		Cone 10 Reduction

NCSU Craft Center

Kaolin	20		Dawn Hoyle

Ball Clay	20

Nephelyne Syenite	25

Flint (Silica)	30

Borax	 5

Brown:

Red Iron Oxide	40

Rutile	10

Blue:

Chrome	 4

Cobalt Oxide	 3

White:

Tin Oxide	 7

Borax	 5

Golden:

Rutile	10

Gerstley Borate	10

Black:

Cobalt Oxide	 5

Red Iron Oxide	22

Manganese Dioxide	16

Green:

Chrome	40

Cobalt Carbonate	30

Yellow:

Rutile	40

Use on leather hard or bisque.  Make thinner for bisque.  Dawn uses the green and yellow, thinned down like watercolors, on top of glazes.

Golden Slip		Cone 10 Reduction

Dawn Hoyle

Rutile	10

Gerstley Borate	10

EPK	 2

Minnis' Slips		Cone 10

Sherry Nicholson

Brown:

Albany Slip	70

Red Iron Oxide	30

Rutile:

(Pink in oxidation, yellow in reduction)

Rutile	30

Albany Slip	70

Blue:

Cobalt Carbonate	 5

Albany Slip	95

Black:

Albany Slip	90

Manganese Dioxide	10 --

Chrome	10   |- or  Black Glaze stain

Copper Oxide	10 --

Sherry uses on leather hard greenware.

Dawn uses the brown on top of glaze (thinned down).

CLAY BODIES

Penland Porcelain		Cone 10

Mary Roehm

Tile 6 Kaolin	200 lb.		Ed Duffield

Ball Clay	 35 lb.

NC4 Feldspar	120 lb.

Silica	100 lb.

Pyrotrol (porcelain grog)	 40 lb.

Bentonite	  8 lb.

Penland Stoneware		Cone 10

Mary Roehm

A P Green fire clay	400 lb.	  Ed Duffield

Ball Clay	225 lb.

NC4 Feldspar	 30 lb.

Burnsred (ocmulgee)	 75 lb.

Grog	 25 lb.

NOTES AND TIPS

Marking Ink			Dawn Hoyle

Cobalt Oxide	1.5 tsp.

Red Iron Oxide	1.0 tsp.

Chrome Oxide	0.5 tsp.

Mix in enough water to make the consistency of ink.  I use this to sign my pots - it's black.  Also good for marking test pots.

Kiln Wash			Dawn Hoyle

Kaolin	20%

Flint	80%

To apply - wet shelf, then brush on several coats in opposite directions.  Not necessary to dry between coats.

Easy Way to Mix Glazes			Dawn Hoyle

Measure and mix dry ingredients in a covered container.  Pour it into another container with water in it.  (I usually step outside to do this part, if possible, and wear a mask.)  Leave for about an hour and allow dry ingredients to become moist.  Then stir (I use a Jiffy mixer), strain several times and adjust water for correct consistency.

ALPHABETICAL LIST OF GLAZES

"A" Glaze	50

Albany Dark Brown	10

Alfred L. Celadon	12

Alice	32

Alp	32

Aurora Copper Luster	19

Beautiful Blue	 6

Behren's Spinach Green	28

Best Possible White	50

Birds Beak Blue	 6

Blue Break Up	 6

Blue Olive	 7

Bringle Slip	58

Bringle Yellow	55

Buttercream	24

Buttermilk	24

Celadon	12

Choy Blue Celadon	12

Chuck Hindes Shino	32

Chun Red	45

Clear Glaze	15

Copper Colemanite	19

Copper Luster	19

Copper Matte	19

Copper Red #1	45

Crane	24

Cushing Black	 3

D 9	32

Druckman	32

Edge's White	50

Ferguson White	51

Flambe	45

Flame	41

Foundry Celadon	13

Funny Runny Bunny	46

G 203	46

Georgia Clear	15

Golden Slip	58

Grass Green	28

Guston Shino	33

Honey	33

Honey (Heavy Iron)	33

Hymen's Basic Matte	24

Iron Red	41

Joan's Plum	41

K-10	 3

King Red 1	46

King Red 3	46

Leach's Transparent Base	15

Lithium Glaze	20

Lizard Skin	20

LMG	20

Marianne Green	28

Matte & White	51

Mead	55

Minnis' Slips	59

Moonglow	25

Mustard	55

Oatmeal	25

Ohata Red	41

Orange 1	38

Orange 2 	38

Orange 3	38

Oxblood	47

Oxblood 2	47

Peacock	29

Persimmon	42

Plum	42

Pumpkin	33

Pumpkin	34

Raku Base Glaze	16

Raku Transparent	16

Red #1	47

Red #2	47

Reitz Orange	38

Rhodes Black	 3

Satin Doll	 3

Shaner Orange	39

Shino #3	34

Shino #5 	34

Simmon	34

SLG 25 Tan	25

SLG 30 Matte	25

SLG 30 Satin	25

Stanley Base Glaze	34

Stoney Matt	35

T-14 Celadon	13

Tan	25

Temokuse	42

Temple White	51

#13 Transparent	16

Turner Blue	 7

Val's Copper Luster	20

Vera Blue	 7

Weiser Rust	21

White Liner	52

Willie Hillix	21

Yanagihara	35

INDEX 1 - GLAZES BY COLOR

Black

Copper Colemanite 	 19

Cushing Black 	 3

K-10 	 3

Rhodes Black 	 3

Satin Doll 	 3

Stanley Base Glaze 	 35

Willie Hillix 	 21

Blue

"A" Glaze 	 50

Beautiful Blue 	 6

Behrens Spinach Green 	 28

Birds Beak Blue 	 6

Blue Break Up 	 6

Blue Olive 	 7

Choy Blue Celadon 	 12

Copper Colemanite 	 19

Georgia Clear 	 15

Leach's Transparent Base 	 15

Peacock 	 29

Stanley Base Glaze 	 35

Temple White 	 51

Turner Blue 	 7

Vera Blue 	 7

Willie Hillix 	 21

Brown

"A" Glaze 	 50

Albany Dark Brown 	 10

Behrens Spinach Green 	 28

Stanley Base Glaze 	 35

Celadon

Alfred L.Celadon 	 12

Celadon (NCSU) 	 12

Choy Blue Celadon 	 12

Foundry Celadon 	 13

Leach's Transparent Base 	 15

T-14 Celadon 	 13

Clear/Transparent

#13 Transparent 	 16

Clear Glaze 	 15

Georgia Clear 	 15

Leach's Transparent Base 	 15

Raku Base Glaze 	 16

Raku Transparent 	 16

Copper

"A" Glaze 	 50

Aurora Copper Luster 	 19

Copper Colemanite 	 19

Copper Luster 	 19

Copper Matte 	 19

Lithium Glaze 	 20

Lizard Skin 	 20

LMG 	 20

Val's Copper Luster 	 20

Weiser Rust 	 21

Willie Hillix 	 21

Cream/Off-white

"A" Glaze 	 50

Buttercream 	 24

Buttermilk 	 24

Crane 	 24

Hymen's Basic Matte 	 24

Moonglow 	 25

Oatmeal 	 25

SLG 25 Tan 	 25

SLG 30 Matte 	 25

SLG 30 Satin 	 25

Tan 	 25

Green

"A" Glaze 	 50

Alfred L.Celadon 	 12

Behrens Spinach Green 	 28

Celadon 	 12

Copper Colemanite 	 19

Grass Green 	 28

Marianne Green 	 28

Peacock 	 29

Stanley Base Glaze 	 35

Val's Copper Luster 	 20

Willie Hillix 	 21

Orange

Guston Shino 	 33

Orange 1 	 38

Orange 2 	 38

Orange 3 	 38

Reitz Orange 	 38

Shaner Orange 	 39

Pink

Funny Runny Bunny 	 46

Stanley Base Glaze 	 35

Red

Flame 	 41

Iron Red 	 41

Joan's Plum 	 41

Ohata Red 	 41

Persimmon 	 42

Plum 	 42

Temokuse 	 42

Willie Hillix 	 21

Red (Copper)

Chun Red 	 45

Copper Red 	 45

Flambe 	 45

Funny Runny Bunny 	 46

G 203 	 46

King Red 1 	 46

King Red 3 	 46

Oxblood 	 47

Oxblood 2 	 47

Red #1 	 47

Red #2 	 47

Turquoise

Copper Colemanite 	 19

White

"A" Glaze 	 50

Best Possible White 	 50

Edge's White 	 50

Ferguson White 	 51

Guston Shino 	 33

Leach's Transparent Base 	 15

Matte & White 	 51

Stanley Base Glaze 	 35

Temple White 	 51

White Liner 	 52

Yellow

Bringle Yellow 	 55

Hymen's Basic Matte 	 24

Mead 	 55

Mustard 	 55

Stanley Base Glaze 	 35

INDEX 2 - GLAZES BY TEMPERATURE/FIRING METHOD

Cone 4-5 Oxidation

Copper Colemanite 	 19

Cone 5-6 Oxidation

"A" Glaze 	 50

Behrens Spinach Green 	 28

Blue Break Up 	 6

Cone 6 Oxidation

Beautiful Blue 	 6

LMG 	 20

Matte & White 	 51

Cone 7-9 Oxidation

Stanley Base Glaze 	 34

Cone 9-10 Oxidation

Bringle Yellow 	 55

Crane 	 24

Oatmeal 	 25

Cone 10 Oxidation

Blue Olive 	 7

Hymen's Basic Matte 	 24

Pumpkin 	 34

Cone 9-10 Reduction

Bringle Yellow 	 55

Crane 	 24

Cushing Black 	 3

Leach's Transparent Base 	 15

Oatmeal 	 25

Satin Doll 	 3

Shaner Orange 	 39

Cone 10 Reduction

#13 Transparent 	 16

Albany Dark Brown 	 10

Alfred L. Celadon 	 12

Alice 	 32

Alp 	 32

Best Possible White 	 50

Birds Beak Blue 	 6

Blue Olive 	 7

Bringle Slip 	 58

Buttercream 	 24

Cone 10 Reduction (cont.)

Buttermilk 	 24

Celadon 	 12

Choy Blue Celadon 	 12

Chuck Hinds Shino 	 32

Chun Red 	 45

Copper Red #1 	 45

D 9 	 32

Druckman 	 32

Ferguson White 	 51

Flambe 	 45

Flame 	 41

Foundry Celadon 	 13

G 203 	 46

Georgia Clear 	 15

Golden Slip 	 58

Grass Green 	 28

Guston Shino 	 33

Honey 	 33

Hymen's Basic Matte 	 24

Iron Red 	 41

Joan's Plum 	 41

K-10 	 3

King Red 1 	 46

King Red 3 	 46

Marianne Green 	 28

Mead 	 55

Moonglow 	 25

Mustard 	 55

Ohata Red 	 41

Orange 1 	 38

Orange 2 	 38

Orange 3 	 38

Oxblood 	 47

Oxblood 2 	 47

Peacock 	 29

Persimmon 	 42

Plum 	 42

Pumpkin 	 33, 34

Red #1 	 47

Red #2 	 47

Reitz Orange 	 38

Rhodes Black 	 3

Shino #3 	 34

Shino #5 	 34

Simmon 	 34

SLG 25 Tan 	 25

SLG 30 Matte 	 25

SLG 30 Satin 	 25

Stoney Matte 	 35

T-14 Celadon 	 13

Tan 	 25

Temokuse 	 42

Temple White 	 51

Turner Blue 	 7

Vera Blue 	 7

Cone 10 Reduction (cont.)

White Liner 	 52

Willie Hillix 	 21

Yanagihara 	 35

Raku

Aurora Copper Luster 	 19

Clear Glaze 	 15

Copper Luster 	 19

Copper Matte 	 19

Edge's White 	 50

Lithium Glaze 	 20

Lizard Skin 	 20

Raku Base Glaze 	 16

Raku Transparent 	 16

Val's Copper Luster 	 20

Weiser Rust 	 21

Salt

Funny Runny Bunny 	 46

Honey 	 33